## Slide 1
Characteristics of Degree of Compaction and Stiffness of Two Different Embankment Slopes:
A Case Study
Dr. Suman Manandhar, Tribhuvan University, Nepal
Noriyuki Yasufuku, Kyushu University, Japan
Ranjan Kumar Dahal Tribhuvan University, Nepal
Mitsuru Taniyama, Asakawagumi Co., Japan
Assistant Professor,
Geodisaster Research Center, Central Department of Geology, Tribhuvan University, Kirtipur, Kathmandu, NEPAL
Visiting Faculty,
School of Engineering, Department of Civil & Geomatic Engineering, Kathmandu University, NEPAL
Visiting Associate Professor
Institute of Lowland and Marine Research (ILMR), Saga University, JAPAN
Secretary General cum Treasurer
International Association of Lowland Technology (IALT), JAPAN
Associate Editor & Chief Guest Editor
Lowland Technology International Journal (LTI), JAPAN
Secretary
Nepalese Society of Engineering Geologist (NSEG), NEPAL
EGCON-2018,
4 December, 2018

## Slide 2: Characteristics of Degree of Compaction and Stiffness of Two Different Embankment Slopes: A Case Study
Phases
Site Investigation and Results of First Embankment
Results of Modified Second Embankment
Monitoring and Effects of Materials

## Slide 3
Phase 1
Preliminary Site Investigation and its Results
Objective
Understand the general behavior of medium-sized embankment constructed by the Construction Company

## Slide 4: Embankment Site
The embankment was built with a Smooth Roller Compactor.
Slope was built with a Bucket of excavator.
Iwade Shi
Wakayama Prefecture
Slope-D

## Slide 5: Compaction Devices
TW500W-1 Sakai Smooth Roller Compactor
Komatsu PC 120-6 Excavator

## Slide 6
X
Y
Z
Slope was recreated with increasing number of tamping blow
24 blows
36 blows
48 blows
4.2 m
4.2 m
8 Passes
12 Passes
16 Passes

## Slide 7
JGS classification | GFS
Uc | 393.94
D50, mm | 1.0
dmax, g/cm3 | 1.975
wopt, % | 8.5
w, % | 18.3
JIS A 1210
JGS 0711
Method of Compaction: E-c
Preparation of specimen: Wet
Procedure of compaction: Non repeated
Weight of rammer: 4.5 kg
Height of fall: 45 cm
Blow per layer: 92
Number of layer: 3

## Slide 8: Field Equipment
Falling Weight Defletometer (FWD)
Moisture Density Gauge (RI)

## Slide 10
Triangulation Model
The Triangulation model shows that higher water content decreases stiffness for the same degree of compaction.

## Slide 11
Phase 2
Results of Modified Second Embankment
Objective
Assess the quality based on time effect monitoring and settlement with changing number of tamping blows

## Slide 12: New and Modified Embankment
R1
R2
R3
BUCKET-TAMPING
Kainan Shi
Wakayama Prefecture
L
M
N
5 Blows
15 Blows
30 Blows

## Slide 13: Material Property
Local natural soils with rock fragments
JGS classification of soil | GFS
Uc | 942.9
D50, mm | 1.3
dmax, g/cm3 | 2.03
wopt, % | 8.7
Natural water content, w, % | 13.65
JIS A 1210
JGS 0711
Method of Compaction: E-c
Preparation of specimen: Wet
Procedure of compaction: Non repeated
Weight of rammer: 4.5 kg
Height of fall: 45 cm
Blow per layer: 92
Number of layer: 3

## Slide 14: Pre-molded embankment slope
Sectional and plan view of pre-molded embankment slope
Grid were made for pre-molded slopes for data measurement

## Slide 15: Grid to measure pre-molded embankment slope

## Slide 16: Static Compaction
Bucket Tamping Method
  Slope-L: 5 uniform blow of tamping
  Slope-M: 15 uniform blow of tamping
  Slope-N: 30 uniform blow of tamping
  Grid were developed to perform the tests of soil stiffness (FWD), dry density (RI), and sampling (Water content)

## Slide 17
Highly scattered Dc lied under 95%; maximum in between 80-85 %.

## Slide 18
Averaged degree of compaction lies in between 80-90%.

## Slide 19
Slope-L: Number of Tamping Blow = 5
Slope-M: Number of Tamping Blow = 15
Slope-N: Number of Tamping Blow = 30
Relative Compaction (RC): 95 %
RC: 90 %
RC: 80 %
(wav= 8.8 %)
(9.2%)
(9.1%)
wav= Average water content
Averaged relative degree of compaction increases from 82-88%.

## Slide 20
Average soil stiffness slightly increased.
Slope-L: Number of Tamping Blow = 5
Slope-M: Number of Tamping Blow = 15
Slope-N: Number of Tamping Blow = 30
(wav= 8.8 %)
(9.2%)
(9.1%)
wav= Average water content

## Slide 21
L2
12回
M2
24回
N2
50回
L
5回
M
15回
N
30回
New slopes
Settlement

## Slide 22
H=50 cm
Height of tamping
Increasing degree of compaction increased stiffness.
Wopt = 8.7 %
Wopt = 8.7 %

## Slide 23
R-1: Number of Passing = 8
R-2: Number of Passing = 16
R-3: Number of Passing = 30
Average dry density improved in between 90-95%.
Relative Compaction (RC): 95 %
RC: 90 %
RC: 80 %
(wav= 6.6 %)
(10.6 %)
(10.7 %)
wav= Average water content

## Slide 24: Monitoring as a Time Effect
Quality improves with negligible fluctuations of water content.

## Slide 26
Rainfall decreased stiffness and degree of compaction.

## Slide 27
s = 9 cm
s = 9 cm
s = 7 cm
Settlement
L2: 12回
s = 11 cm
s = 11 cm
s = 10 cm
Settlement
M2: 24回
s = 14 cm
s = 13 cm
s = 13 cm
Settlement
N2: 50回
前回の条件
L’: 12回
M’: 2４回
N’: 50回
L2
12回
M2
24回
N2
50回
L
5回
M
15回
N
30回
今回の代わった載り面
Settlement Before Rainfall
January, 2012

## Slide 28
s = 7 cm
s = 6 cm
s = 7 cm
Settlement
L2: 12回
s = 7 cm
s = 7 cm
s = 6 cm
Settlement
M2: 24回
s = 8 cm
s = 7 cm
s = 6 cm
Settlement
N2: 50回
前回の条件
L2
12回
M2
24回
N2
50回
L
5回
M
15回
N
30回
代わった載り面
April, 2012
Settlement After Rainfall

## Slide 29
Maximum 14 cm settlement achieved about 90% degree of compaction during bucket tamping method.

## Slide 30
Rainfall decreased less than 90% degree of compaction and stiffness during bucket tamping method after rainfall.

## Slide 31
Why Dc and Kf decreased?
Phyllitic rock particles affect the degree of Dc and Kf even with slight rain trickles.
Phyllite
Due to lack of adequate knowledge on engineering geological characteristics of materials used for the construction.

## Slide 32
Conclusions
Monitoring of slopes and top of the embankment show the increase in degree of compaction and soil stiffness.
The degree of compaction increased near dry side of the optimum water content.
Near or more than 90% degree of compaction can be achieved if half of the total thickness of soil layer is settled down during bucket tamping method.
The Triangulation model shows that higher water content decreases stiffness for the same degree of compaction.
Phyllitic rock particles affect the degree of Dc and Kf even with slight rain trickles

## Slide 33
Thank You very much
for your kind attention!!!
EGCON-2018,

## Slide 36: Compaction Mold
Size：4.75mm passing
Diameter of the mold:28.6 cm,
Height of the mold:30 cm
Weight of rammer：4.5 kg
No. of layer：5 layers/1per 6 cm
No. of blow：216/layer
28.6cm
30cm
6cm/layer
ＥＣ：Energy(kJ/m3)
ＷＲ：Weight of rammer (kN)
Ｈ：Height of rammer (m)
ＮＢ：Number of blow
ＮＬ：Number of layer
Ｖ：Volume of compacted soil (m3)

## Slide 37: Moisture-Density curve

## Slide 38: Results at same water content
dmax:1.88g/cm3
wopt:13.3%

## Slide 39: Coefficient of FWD variation on moisture-density curve
Stiffness and compaction can be increased with increasing compaction energy.
FWD係数=1000
FWD係数=500
dmax:1.88g/cm3
wopt:13.3%

## Slide 40
Phases
Preliminary Site Investigation and its Results
New and Modified Embankment
Innovation of New Devices
1
2
3

## Slide 41
Phase 3
Innovation of New Device
Objective
Develop a new device based on different compaction methodology and make able to innovate Real Time Measurement System

## Slide 42: New Devices
80 cm
50 cm

## Slide 43
Vibro-Compaction Method
Time (sec)
0 s
3 s
6 s
9 s
15 s
30 s

## Slide 44
High compaction with high stiffness lies in between 6s &15 s vibration time.
Results

## Slide 45
With increasing duration of vibro-compaction in the slope, dry density increases.

## Slide 46
Innovation of Device for Static compaction

## Slide 48: Installation of pressure cells and results on recreated slopes

## Slide 52
Expected line of pressure increment

## Slide 53
Expected line of pressure increment
Average pressure distribution for slopes. Pressure is expected to be increased with increasing compaction energy.

## Slide 54
Expected line of pressure increment
Average pressure distribution with increasing tamping energy with expected increment trend of pressur with increasing compaction energy.
(83.9 %)
(82.8 %)
(84.7 %)

## Slide 55
Future Strategy
Innovate laboratory scale compaction device

## Slide 56
Future Strategy
Innovate laboratory scale compaction device

## Slide 57
Conclusion of Phase 1
The Triangulation model shows that higher water content decreases stiffness for the same degree of compaction.
Preliminary Site Investigation and its Results

## Slide 58
Conclusion of Phase 2
Monitoring of slopes and top of the embankment show the increase in degree of compaction and soil stiffness.
New and Modified Embankment
Conclusion
The degree of compaction increased near dry side of the optimum water content.
Near or more than 90 % degree of compaction can be achieved if half of the total thickness of soil layer is settled down during bucket tamping method.

## Slide 59
Conclusion of Phase 3
Conclusions
Vibro-compaction shows that higher degree of compaction and stiffness can be achieved in between time interval of 6 seconds and 15 seconds.
Innovation of New Device

## Slide 60
Thank You very much
for your kind attention!!!